GUARDRAIL DELINETORS					May 16, 2006

The following specifications are for the purchase of Flexible Guardrail Delineators.

Delineators shall meet current KDOT specifications and be NCHRP - 350 compliant.

They shall have approximately 8 square inches of reflectivity.  The shape of the delineators shall allow them to fit within the channel of the guardrail.  Brackets shall be manufactured from high impact polycarbonate with a smooth, high gloss finish.  Brackets shall be approximately .085 inches thick, 5 inches in width, and 3” tall.  Reflective sheeting shall be prismatic high intensity.

Slip on style shall have a slot on the base that will fit over a standard size guard rail bolt.  The glue on style shall have holes drilled or cast into the material to improve adhesion.

Product shall be AKT Corporation Model 717-1 and 721-1 or approved equal.